## Slide 1
数値シミュレーションレーションによる
粉末金型充填における吸引効果の影響
○吉田昂生1, 森勇稀1,高畑和弥1 酒井幹夫2*
1. 東京大学大学院工学系研究科原子力国際専攻
化学工学会関東支部横浜大会
分類 : 6-f 情報処理技術
2019/8/8
2. 東京大学大学院工学系研究科レジリエンス工学研究センター

## Slide 2: 研究背景
・粉末金型充填
錠剤の生産プロセスの一部。充填の後に圧縮・排出を経て錠剤は生産されている。
粉末は充填中に空気抵抗を受けるため、充填には時間がかかりプロセス全体のネックになっている。
Tablet
(www.pakutaso.com)
Rotary Tablet Press Machine
(Copyright © 2003 HATA TEKKOSHO CO.,LTD. All rights reserved.)
・吸引効果
粉末の下に設置した杵を降下させることにより粉末が金型内に引き込まれる効果。
充填速度の改善効果があるとされている。

## Slide 3: 先行研究・本研究の目的
Air pressure gradient accelerated the flux of powder flow and shortened the filling time [1] . But how pressure gradient affected the powder filling has not been clarified so far.
The moving speed of the lower punch is one of the key factor of the suction filling performance. But quantitative data has not been obtained, because it is difficult to get it experimentally.
1. How does the suction effect influences the powder?
2. Influence of the moving speed of the lower punch for the filling time
[1] C.-Y. Wu et al, Chem. Eng. Sci. (2012)
Reveal concretely how air pressure gradient influences the powder filling.
Reveal the influence of the moving speed of the lower punch for the filling time.
Air Pressure [1]
Notes: It could be assumed that air pressure gradient accelerated the influx of the powder and shortened the filling time [1] .
But how pressure gradient affected the powder movement has not been clarified so far.

## Slide 4: Numerical Method
・Modeling of solid phase and gas phase
In this study, for modeling solid-gas phase interaction DEM-CFD method[1] (Discrete Element Method - Computational Fluid Dynamics) was used. (Particles are modeled by DEM, Air is modeled by CFD)
[1] Y. Tsuji et al., Powder Tec. (1993).
[2] Y. Shigeto and M. Sakai, Chem. Eng. J. (2013).
・Boundary Conditions
In this study, we used Signed Distance Function[2] and Immersed Boundary Method[3] combinedly to calculate moving boundary in gas-solid flow. Only with simple algorithms, this combination enable to calculate interaction with wall in arbitrary shape. This combination of boundary conditions had verified.[4][5]
Solid Phase : SDF (Signed Distance Function)
Gas Phase : IBM (Immersed Boundary Method)
SDF Field
[3] C.S. Peskin, J. Comput. Phys. (1972).
[4] Y. Mori et al., Powder Tec. (2019).
Gas Phase
Wall Region
IBM Field
[5] H. Yao et al., J. Taiwan Inst. Chem. Eng. J. (2018).
+
Notes: 5分
Signed Distance Function
Boundary is defined by the scalar field of the distance from wall. With this scalar field, it is easy to calculate the interaction between a particle and a wall.
ImmersedBoundary Method
The interaction between the gas phase and a wall is calculated only by ratio of the wall in a staggered grid. The ratio is obtained easily by Signed Distance Function.
This combination of boundary conditions enables it easy to calculate interaction with wall in arbitrary wall shape, only with very simple algorithms.

## Slide 5
How Does the Suction Effect Influences the Powder?

## Slide 6: Simulation Conditions
To understand the influence of suction effect, compare the suction filling with the gravity filling.
 | Case 1-1 | Case 1-2
Filling Type | Suction Filling* | Gravity Filling
* Punch Lower Velocity = 300 [mm/s]
Gas phase | 
Viscosity | [Pa・s]
Density | 1 [kg/m3]
Solid phase | 
Density | 1500 [kg/m3]
Spring constant | 50 [N/m]
Coefficient of restitution | 0.9
Coefficient of friction | 0.3
Gas phase | 
Viscosity | 
Density | 1 [kg/m3]
Solid phase | 
Density | 1500 [kg/m3]
Spring constant | 50 [N/m]
Coefficient of restitution | 0.9
Coefficient of friction | 0.3
Diameter of particles | 250 [μm]
Number of particles | 500,000
System | Mono-dispersed
Grid size | 0.5 [mm]
Calculation time | 0.24 [s]
Physical Properties
Calculation Conditions
Punch
Schematic Geometry
Unit : mm
Initial Position of Particles

## Slide 7: Results & Discussion (Effect of punch movement)
Case 1-1
Suction Filling
Case 1-2
Gravity Filling
Suction effect accelerated the flux of powder flow
Case 1-1
Suction Filling
Case 1-2
Gravity Filling

## Slide 8: Results & Discussion (Air Pressure Gradient)
Case 1-1
Suction Filling
Case 1-2
Gravity Filling
Case 1-1
Suction Filling
Case 1-2
Gravity Filling
Only at the moment of the punch started moving down
0.002s
0.020s
0.010s
originality

## Slide 9
0.174 s
Approx. 83%
0.210 s
In case suction, powder filling took 83% time compared with case gravity. The suction effect shortened the powder filling time.
The times particles had filled 99% in each case are written.
In case suction, the flux of powder flow increased rapidly compared with case gravity. The suction effect accelerated the flux of powder.
Results & Discussion (Quantitative Evaluation)
The flux increased rapidly and the filling time was shortened
Flux of Particles [1/s・mm2]
Notes: 9, 10分ぐらいで、このCaseが終了したらいいかんじ。

## Slide 10
Influence of the Moving Speed of the Lower Punch

## Slide 11: Simulation Conditions
 | Case 2-1 | Case 2-2 | Case 2-3
Speed of Lower Punch [mm/s] | 100 | 200 | 300
To understand the influence of the moving speed of lower punch in the suction filling, compare 3 cases.
Gas phase | 
Viscosity | [Pa・s]
Density | 1 [kg/m3]
Solid phase | 
Density | 1500 [kg/m3]
Spring constant | 50 [N/m]
Coefficient of restitution | 0.9
Coefficient of friction | 0.3
Gas phase | 
Viscosity | 
Density | 1 [kg/m3]
Solid phase | 
Density | 1500 [kg/m3]
Spring constant | 50 [N/m]
Coefficient of restitution | 0.9
Coefficient of friction | 0.3
Diameter | 250 [μm]
Number of particles | 500,000
System | Mono-dispersed
Grid size | 0.5 [mm]
Calculation time | 0.24 [s]
Physical Properties
Calculation Conditions
Punch
Schematic Geometry
Unit : mm
Initial Position of Particles

## Slide 12
Case 2-1
100 mm/s
Case 2-2
200 mm/s
Case 2-3
300 mm/s
Case 2-1
100 mm/s
Case 2-2
200 mm/s
Case 2-3
300 mm/s
Powder had followed to the punch in each speed
Results & Discussion (Effect of punch movement)

## Slide 13
0.186 s
Approx. 76%
0.228 s
In case 200 and 300 mm/s, powder filling took 82% and 76% time respectively compared with case 100 mm/s. As the punch speed was higher, the filling time was shorter.
As the punch speed was higher, the flux increased rapidly. It is quantitatively suggested that higher punch velocity accelerated the flux of powder flow.
0.174 s
Approx. 82%
Higher punch speed accelerated the flux and shorten the filling time
Flux of Particles [1/s・mm2]
The times particles had filled 99% in each case are written.
originality
Results & Discussion (Quantitative Evaluation)

## Slide 14: Results & Discussion (Void Fraction)
Case 2-2
200 mm/s
Case 2-3
300 mm/s
Rising bubble prevented the flux of powder flow
0.040s
0.080s
Case 2-2
200 mm/s
Case 2-3
300 mm/s
Case 2-1
100 mm/s

## Slide 15: Conclusions
The pressure gradient occurred above the punch moving down. It suctions powder onto the punch and made the path of powder which had accelerated the flux of powder flow.
1. How does the suction effect influences the powder?
2. Influence of the moving speed of lower punch for the filling time
Air pressure gradient influenced to the powder only at the moment of the punch started moving down.
As the moving speed of lower punch was higher, the filling time was shorter.
Higher punch velocity accelerate the influx of powder and shorten the filling time. After punch had finished moving down, bubble started rising and prevented the flux of powder flow.
originality
originality
Notes: 12分

## Slide 16
As the punch velocity is higher, the vortex in the die became larger. And it looked like limiting the path of the powder flux.
Case 2-1
100 [mm/s]
Case 2-2
200 [mm/s]
Case 2-3
300 [mm/s]
Vector of air flow (0.08 [s])
Higher punch velocity made the larger vortex
The time shortened by the increase of velocity had gradually decreased. It shows that something prevented the influx of powder.
originality
0.042s
0.012s
Results & Discussion
Notes: 11分

## Slide 17: Conclusions
The pressure gradient occurs above the punch when it start lowering. It suctions powder onto the punch and make the path of powder which has accelerate the influx of powder.
1. How does the suction effect affect the powder
2. Influence of the lower punch velocity for the filling time
Air pressure gradient affects to the powder only at the moment of the punch start lowering.
As the punch velocity is higher, the filling time is shorter, but the effect gradually decreases.
Higher punch velocity accelerate the influx of powder. But it creates the larger spiral flow which makes path of the powder narrow. It is suggested that this is one of the reason that the suction effect for filling time gradually decreases as punch velocity is higher.
originality
originality
Notes: 12分

## Slide 18
As the punch velocity is higher, the spiral flow in the die became larger. And it looked like limiting the path of the powder flux.
Case 2-1
100 [mm/s]
Case 2-2
200 [mm/s]
Case 2-3
300 [mm/s]
Vector of air flow
(when overlapping started)
Higher punch velocity creates the larger spiral flow
Discussion (Results & Discussion)
originality
Case 2-2
200 [mm/s]
Case 2-3
300 [mm/s]
Notes: 11分

## Slide 19: Numerical Method
Solid Phase : DEM[2]
Gas Phase : CFD + Local Average Volume3]
+
Exchange of momentum
[1] Y. Tsuji et al., Powder Tec. (1993).
[2] P.A. Cundall and O.D. Strack, Geotechnique (1979)
[3] T.B. Anderson and R. Jackson, Ind. Eng. Chem. Fundam. (1967)
・Modeling of solid phase and gas phase
In this study, for modeling solid-gas phase interaction DEM-CFD method[1] (Discrete Element Method - Computational Fluid Dynamics) was used. (Particles are modeled by DEM, Air is modeled by CFD)

## Slide 20: Numerical Method
Solid Phase : SDF[1]
Gas Phase : IBM[2]
[1] Y. Shigeto et al, Chem. Eng. J. (2013).
[2] C.S. Peskin, J. Comput. Phys. (1972).
+
Signed Distance is changing with wall moving
・Boundary Conditions
In this study, we used Signed Distance Function[2] and Immersed Boundary Method[3] combinedly to calculate moving boundary in gas-solid flow. This combination of boundary conditions had verified.[4][5]