## Slide 1
数値シミュレーションによる
粉末金型充填における吸引効果の影響
○吉田昂生1 森勇稀1 高畑和弥1 酒井幹夫2*
1. 東京大学大学院工学系研究科原子力国際専攻
化学工学会関東支部横浜大会
横浜国立大学
2019/8/8
2. 東京大学大学院工学系研究科レジリエンス工学研究センター

## Slide 2: 研究背景
下杵の降下により粉末の充填を促す効果。
吸引効果がどのように作用しているのか明らかでない。
・粉末金型充填
錠剤などの成型プロセスの一部。
プロセス全体の時間的ボトルネック。
Tablet
Rotary Tablet Press Machine
(Copyright © 2003 HATA TEKKOSHO CO.,LTD. All rights reserved.)
・吸引効果
[1] S. Jackson, I.C. Sinka, A.C.F. Cocks, 2006
[2] C. –Y. Wu, Y. Guo, 2012
下杵の降下はその上部と粉末の間に低圧領域をつくりだしていることが実験により明らかにされた。 [1] [2]
✔ 低圧領域をつくりだす
低圧領域ができることによって粒子にどのように力が作用するのかが明らかにされていない。
✗ 力の作用の仕方が不明
吸引効果において重要とされている下杵の降下速度への依存性が明らかにされていない。
✗ 下杵の降下速度への依存性が不明
問題点

## Slide 3: 本研究の目的
吸引効果の作用を数値シミュレーションを用いて分析する
✎ 本研究の目的
✗ 実験では分析が難しい
・センサの干渉や体系の小ささにより実験では現象の観測が難しい
・下杵の降下速度を任意の値に設定することが難しい
・センサの設置が不要
・下杵の降下速度を任意の値に設定することができる
✔ 数値シミュレーションなら分析できる

## Slide 4: 解析条件
下杵の降下速度をパラメータとし100, 200, …, 700 mm/s の7ケースを比較
Gas Phase | 
Viscosity | Pa・s
Density | 1 kg/m3
Solid Phase | 
Density | 1500 kg/m3
Spring Constant | 50 N/m
Coefficient of restitution | 0.9
Coefficient of friction | 0.3
Gas Phase | 
Viscosity | 
Density | 1 kg/m3
Solid Phase | 
Density | 1500 kg/m3
Spring Constant | 50 N/m
Coefficient of restitution | 0.9
Coefficient of friction | 0.3
Diameter | 250 μm
Number of particles | 500,000
System | Mono-dispersed
Grid size | 0.5 mm
Calculation time | 0.24 s
物性値
計算条件

## Slide 5: 結果・考察
100 mm/s
300 mm/s
500 mm/s
700 mm/s
充填量に差がない
速度が大きいと粒子も空気も多く入り込む
粒子の流入の様子を視覚的に確認できた
側面部分に空気が溜まっている

## Slide 6: 結果・考察
下杵の降下速度に比例した大きさのピーク
大きさがばらばらのピーク
吸引効果によりフラックスに2つのピークがでる
フラックスを観測している面

## Slide 7: 結果・考察
速度に比例して流体抗力と圧力勾配による力が大きい
originality
100 mm/s
300 mm/s
500 mm/s
700 mm/s
流体抗力
圧力勾配による力
重力
下杵の降下開始時
(0.02s)

## Slide 8: 結果・考察
空気が粒子の流入路を狭めている
流入路が細くなりフラックスが低下する
originality

## Slide 10: 結論
下杵降下開始の瞬間に流体抗力および圧力勾配による力で粒子が金型内に引き込まれる。
下杵の降下速度が大きいほど粒子に強い力がかかる。
1. 下杵降下開始の瞬間に大きな力が粒子に加わる
粒子の流入路は金型内に溜まった空気により狭められ流入量が落ちる原因となる。
下杵の降下速度が大きいほど狭められる。
2. 粒子の流入路が空気により狭められる
吸引効果の作用

## Slide 11: 解析手法
✗ 移動する壁面の扱いが難しい
数値シミュレーションにおいて、移動する壁面の境界条件は複雑になりやすく、扱いが難しい。
埋め込み境界法[1]
[1] C.S. Peskin, 1972
の壁面の割合
速度
流体グリッド内の壁面の割合を用いて流体ー壁面間の相互作用を評価。シンプルなアルゴリズムで計算が可能。
気相の支配方程式
速度
壁面
流体領域
埋め込み境界法で定義されているフィールドが移動する壁面に追従している様子
Notes: 5分
Signed Distance Function
Boundary is defined by the scalar field of the distance from wall. With this scalar field, it is easy to calculate the interaction between a particle and a wall.
ImmersedBoundary Method
The interaction between the gas phase and a wall is calculated only by ratio of the wall in a staggered grid. The ratio is obtained easily by Signed Distance Function.
This combination of boundary conditions enables it easy to calculate interaction with wall in arbitrary wall shape, only with very simple algorithms.

## Slide 12: Numerical Method
Solid Phase : DEM[2]
Gas Phase : CFD + Local Average Volume3]
+
Exchange of momentum
[1] Y. Tsuji et al., Powder Tec. (1993).
[2] P.A. Cundall and O.D. Strack, Geotechnique (1979)
[3] T.B. Anderson and R. Jackson, Ind. Eng. Chem. Fundam. (1967)
・Modeling of solid phase and gas phase
In this study, for modeling solid-gas phase interaction DEM-CFD method[1] (Discrete Element Method - Computational Fluid Dynamics) was used. (Particles are modeled by DEM, Air is modeled by CFD)

## Slide 13: Numerical Method
Solid Phase : SDF[1]
Gas Phase : IBM[2]
[1] Y. Shigeto et al, Chem. Eng. J. (2013).
[2] C.S. Peskin, J. Comput. Phys. (1972).
+
Signed Distance is changing with wall moving
・Boundary Conditions
In this study, we used Signed Distance Function[2] and Immersed Boundary Method[3] combinedly to calculate moving boundary in gas-solid flow. This combination of boundary conditions had verified.[4][5]

## Slide 14: 解析手法
・Modeling of solid phase and gas phase
In this study, for modeling solid-gas phase interaction DEM-CFD method[1] (Discrete Element Method - Computational Fluid Dynamics) was used. (Particles are modeled by DEM, Air is modeled by CFD)
[1] Y. Tsuji et al., Powder Tec. (1993).
[2] Y. Shigeto and M. Sakai, Chem. Eng. J. (2013).
・Boundary Conditions
In this study, we used Signed Distance Function[2] and Immersed Boundary Method[3] combinedly to calculate moving boundary in gas-solid flow. Only with simple algorithms, this combination enable to calculate interaction with wall in arbitrary shape. This combination of boundary conditions had verified.[4][5]
Solid Phase : SDF (Signed Distance Function)
Gas Phase : IBM (Immersed Boundary Method)
SDF Field
[3] C.S. Peskin, J. Comput. Phys. (1972).
[4] Y. Mori et al., Powder Tec. (2019).
Gas Phase
Wall Region
IBM Field
[5] H. Yao et al., J. Taiwan Inst. Chem. Eng. J. (2018).
+
Notes: 5分
Signed Distance Function
Boundary is defined by the scalar field of the distance from wall. With this scalar field, it is easy to calculate the interaction between a particle and a wall.
ImmersedBoundary Method
The interaction between the gas phase and a wall is calculated only by ratio of the wall in a staggered grid. The ratio is obtained easily by Signed Distance Function.
This combination of boundary conditions enables it easy to calculate interaction with wall in arbitrary wall shape, only with very simple algorithms.

## Slide 15: 結果・考察
充填完了時間と下杵降下速度の関係
フラックスの時間変化
初期のフラックスの大きさで充填完了時間が短くなる
500 mm/sはフラックスの復活が早い
？