## Slide 1
数値シミュレーションレーションによる
粉末金型充填における吸引効果の影響
○吉田昂生1 森勇稀1 高畑和弥1 酒井幹夫2*
1. 東京大学大学院工学系研究科原子力国際専攻
化学工学会関東支部横浜大会
横浜国立大学
2019/8/8
2. 東京大学大学院工学系研究科レジリエンス工学研究センター

## Slide 2: 研究背景
粉末の下に設置した杵を降下させることにより粉末が金型内に引き込まれる効果。吸引効果の影響の定量的な評価は十分になされていない。
・粉末金型充填
錠剤などの成型プロセスの一部。充填の後に圧縮・排出と続く。
充填完了時間の短縮によりプロセスの効率化が期待される。
Tablet
Rotary Tablet Press Machine
(Copyright © 2003 HATA TEKKOSHO CO.,LTD. All rights reserved.)
・吸引効果
Notes: 配置をZ型に

## Slide 3: 先行研究・本研究の目的
自由落下の場合と比較して下杵の降下がある場合に充填完了時間が短縮されることが、実験により明らかにされた。 [1]
下杵の降下速度は充填完了時間に対する重要なパラメータとされている。実験装置の制限、現象の観測の難しさから実験による解析は難しいが、数値シミュレーションならば可能である。
✔ 吸引効果による充填完了時間の短縮が確認
✗ 下杵の降下速度と充填完了時間の関係性
[1] S. Jackson, I.C. Sinka, A.C.F. Cocks, 2006
下杵の降下速度の変化が充填完了時間に及ぼす影響を明らかする
✎ 本研究の目的
Notes: It could be assumed that air pressure gradient accelerated the influx of the powder and shortened the filling time [1] .
But how pressure gradient affected the powder movement has not been clarified so far.

## Slide 4: 解析手法
✗ 移動する壁面の扱いが難しい
数値シミュレーションにおいて、移動する壁面の境界条件は複雑になりやすく、扱いが難しい。
埋め込み境界法[1]
[1] C.S. Peskin, 1972
の壁面の割合
速度
流体グリッド内の壁面の割合を用いて流体ー壁面間の相互作用を評価。シンプルなアルゴリズムで計算が可能。
気相の支配方程式
速度
壁面
流体領域
埋め込み境界法で定義されているフィールドが移動する壁面に追従している様子
Notes: 5分
Signed Distance Function
Boundary is defined by the scalar field of the distance from wall. With this scalar field, it is easy to calculate the interaction between a particle and a wall.
ImmersedBoundary Method
The interaction between the gas phase and a wall is calculated only by ratio of the wall in a staggered grid. The ratio is obtained easily by Signed Distance Function.
This combination of boundary conditions enables it easy to calculate interaction with wall in arbitrary wall shape, only with very simple algorithms.

## Slide 5: 解析条件
下杵の降下速度をパラメータとし100, 200, …, 700 mm/s の7ケースを比較
Gas phase | 
Viscosity | [Pa・s]
Density | 1 [kg/m3]
Solid phase | 
Density | 1500 [kg/m3]
Spring constant | 50 [N/m]
Coefficient of restitution | 0.9
Coefficient of friction | 0.3
Gas phase | 
Viscosity | 
Density | 1 [kg/m3]
Solid phase | 
Density | 1500 [kg/m3]
Spring constant | 50 [N/m]
Coefficient of restitution | 0.9
Coefficient of friction | 0.3
Diameter | 250 [μm]
Number of particles | 500,000
System | Mono-dispersed
Grid size | 0.5 [mm]
Calculation time | 0.24 [s]
物性値
計算条件

## Slide 6: 結果・考察
100 mm/s
300 mm/s
500 mm/s
700 mm/s
充填量に差がない
速度が大きいと粒子も空気も多く入り込む
充填完了時間と下杵降下速度の関係
下杵の降下速度に対して充填完了時間は極小値をとる
originality

## Slide 7: 結果・考察
下杵降下開始時にフラックスが大きい
100 mm/s
300 mm/s
500 mm/s
700 mm/s
速度に比例して圧力勾配が大きくフラックスがあがる
originality

## Slide 8: 結果・考察
充填完了時間と下杵降下速度の関係
フラックスの時間変化
初期のフラックスの大きさで充填完了時間が短くなる
500 mm/sはフラックスの復活が早い
？

## Slide 9: 結果・考察
気泡が分裂して抜けていかない
気泡が塊で抜けていく
下杵の降下速度が大きいと気泡の抜けに時間がかかる
originality

## Slide 10: 結論
下杵の降下速度の変化が充填完了時間に及ぼす影響を明らかする
✎ 本研究の目的
[1] S. Jackson, I.C. Sinka, A.C.F. Cocks, 2006
✔ 充填完了時間はある下杵降下速度で極小値をとる
下杵の降下速度が大きいほど、降下初期に生じる圧力勾配が大きく、粒子が多く流入する。
1. 初期のフラックスの大きさ
下杵の降下速度が大きいほど、充填領域内に大量の空気が流入する。その空気が抜けることに時間がかかる。
2. 流入する空気量の多さ
originality
下杵の降下速度が大きいほど充填完了時間が短くなるというわけではない。それは吸引効果が持つ2つの性質のためである。
Notes: It could be assumed that air pressure gradient accelerated the influx of the powder and shortened the filling time [1] .
But how pressure gradient affected the powder movement has not been clarified so far.

## Slide 11: Numerical Method
Solid Phase : DEM[2]
Gas Phase : CFD + Local Average Volume3]
+
Exchange of momentum
[1] Y. Tsuji et al., Powder Tec. (1993).
[2] P.A. Cundall and O.D. Strack, Geotechnique (1979)
[3] T.B. Anderson and R. Jackson, Ind. Eng. Chem. Fundam. (1967)
・Modeling of solid phase and gas phase
In this study, for modeling solid-gas phase interaction DEM-CFD method[1] (Discrete Element Method - Computational Fluid Dynamics) was used. (Particles are modeled by DEM, Air is modeled by CFD)

## Slide 12: Numerical Method
Solid Phase : SDF[1]
Gas Phase : IBM[2]
[1] Y. Shigeto et al, Chem. Eng. J. (2013).
[2] C.S. Peskin, J. Comput. Phys. (1972).
+
Signed Distance is changing with wall moving
・Boundary Conditions
In this study, we used Signed Distance Function[2] and Immersed Boundary Method[3] combinedly to calculate moving boundary in gas-solid flow. This combination of boundary conditions had verified.[4][5]

## Slide 13: 解析手法
・Modeling of solid phase and gas phase
In this study, for modeling solid-gas phase interaction DEM-CFD method[1] (Discrete Element Method - Computational Fluid Dynamics) was used. (Particles are modeled by DEM, Air is modeled by CFD)
[1] Y. Tsuji et al., Powder Tec. (1993).
[2] Y. Shigeto and M. Sakai, Chem. Eng. J. (2013).
・Boundary Conditions
In this study, we used Signed Distance Function[2] and Immersed Boundary Method[3] combinedly to calculate moving boundary in gas-solid flow. Only with simple algorithms, this combination enable to calculate interaction with wall in arbitrary shape. This combination of boundary conditions had verified.[4][5]
Solid Phase : SDF (Signed Distance Function)
Gas Phase : IBM (Immersed Boundary Method)
SDF Field
[3] C.S. Peskin, J. Comput. Phys. (1972).
[4] Y. Mori et al., Powder Tec. (2019).
Gas Phase
Wall Region
IBM Field
[5] H. Yao et al., J. Taiwan Inst. Chem. Eng. J. (2018).
+
Notes: 5分
Signed Distance Function
Boundary is defined by the scalar field of the distance from wall. With this scalar field, it is easy to calculate the interaction between a particle and a wall.
ImmersedBoundary Method
The interaction between the gas phase and a wall is calculated only by ratio of the wall in a staggered grid. The ratio is obtained easily by Signed Distance Function.
This combination of boundary conditions enables it easy to calculate interaction with wall in arbitrary wall shape, only with very simple algorithms.